## Slide 1: Design of high density SiP
Chris BARRATT
Insight SiP Sophia Antipolis FRANCE
for complex computing system in micro SD format
FRANCE

## Slide 2: Agenda
Introduction
Design Process
  Functional Specification
  Architecture
  Component Choice
  Size versus Component Choice
  Detailed Schematic
  Breadboard
  Substrate Technology
  Layout
  Electromagnetic Simulation
  Assembly
  Test and Debug
Micro SD Linux Computer
“From Sketch to Product”

## Slide 3: Introduction
The Challenge
How to fit a microprocessor and some memory
Inside a Smart Phone
Sorry How to fit a Linux Computer
Inside a Smart Phone

## Slide 4: Functional Specification
Must Fit inside a Smart Phone
Must use micro SD slot
Size 11 x 15 x 1 mm
Interface to Phone via SD interface
Sufficient RAM to run Linux
Sufficient Storage to hold Linux image and programs
Operates from SD power supply
Time to Market
RAM 512MB
Flash 8 GB
MPU
Access via SD port
Runs off 3V from SD

## Slide 5: Architecture
Architecture Choices
  Meet Functional specifications
  Choose off the shelf components (Time to Market)
  Consider solutions which have Linux implementations
2.7V in
3.3V out
1.8V out
1.2V out

## Slide 6: Component Choice
Criteria
  Wafers or WLCSP must be available
    NDA process essential
    Negotiate with Chip Vendors on a project by project basis
    Need to obtain wafer data early to make decisions
  Die sizes must be compatible with Micro SD footprint
  Must meet architecture requirements
  Ideally need EVK with working software stacks for a “breadboard”
  Thickness of WLCSP and SMTs must be compatible with Micro SD (< 0.5 mm)
MPU
Flash
Controller
SD Client
Memories
Power
Supply

## Slide 7: Size vs Component Choice
Evaluate Assembly Options
For each Option estimate size
Choose best compromise
Solution adopted
  4 die Wire Bond Memory stack
    LPDDR2 + 2 NAND Flash
    Flash Controller on LPDDR2
  2 die WB stack MPU On FPGA
  4 WLCSP power supply components
  40 SMT Chips (01005, 0201,..)

## Slide 8: Detailed Schematic
Create a detailed schematic
2 versions are required
  Breadboard with packaged components
  SiP design with bare die components
Optimization of Power supply and decoupling is crucial to fit inside small footprint
  Reduce number of passives from 80 to 40
  Power supply components need to be very small

## Slide 9: Breadboard
Same schematic as SiP
Uses Packaged components
Based on MPU EVK
Allows first level Hardware Debug
Allows Firmware Development to be essentially in parallel with SiP Hardware
Can be used in SiP debug as reference

## Slide 10: Substrate Technology
Requirements
  Wire-bond capable
  100um wire bond finger pitch
  Complex routing  6 layers
  Fine line 30um / 30 um
  Rear side contacts  Hard gold
  As thin as possible <=0.25mm
  Lowest cost option
Solution
  6 layer any layer to any layer
  Electrolytic gold
  Complex plating (buss bar ruled out)
    using 9 process steps
  Pushing limits for etched technology
  Overall substrate very thin (0.22mm)

## Slide 11: Module Layout
Schematic to Layout
Tool-sets
  Cadence Allegro SIP
  Mentor Graphics Xpedition Package Integrator
  Keysight ADS
  Altium PCB
  Other PCB tools
Capability
COST
2D Routing
3D View

## Slide 12: Module Technologies
Die Stacking
  3 dies in < 0.58 mm height
  Die thickness 60 – 80 um
  Film on Wire
  Low loop heights
  Same die size stack
Wire-bonding
  4 layers of wire bonding
  Accurate x y z control to avoid shorts
Small actives
  WLCSP <0.5mm
  DFN < 0.4 mm
Passives
  01005 mostly
  0201 > 100nF
  0402 > 2 uF
  0603 low profile for DC:DC chokes

## Slide 13: Electromagnetic Simulation
Toolset
  Keysight ADS Momentum 2.5D / full 3D FEM
  Ansys HFSS full 3D EM
Substrate Simulation
  Multi-port s parameters (> 100 ports)
  High speed track impedances
  Coupling between power supply and high speed signals
  Effectiveness of decoupling methods (mix EM/Schematic models)
Iterative process
Avoids major failures at first prototype phase
Can be used to fine tune second spin (if needed)
2.5D simulation of Layout
Evaluation of Effects in Schematic

## Slide 14: SiP Assembly
Courtesy of Amkor
SMT placement and reflow
Sequential Die attach – Wire bond
Accurate 3D wire control
Over-molding
  Requires DOE to setup process
Electrical Prototype yield > 95%

## Slide 15: Debug Process
Assumes Breadboard is fully functional
Using Test Board and Socket
  Power Up and Validate Power supplies
  Program MPU with boot sequence and Linux Kernel via JTAG
  Program FPGA with code
  Initialize Flash Controller via MPU
  Boot from Flash
At each step issues can arise
  Compare output with breadboard
  Attempt to put breadboard into same failure mode as SiP
  Attempt to change SMTs in SiP (accurate diamond drilling)
Example
  Issues with assembly spins 1 & 2 was linked to an un-calibrated die and component labelling!!!
  Spin 3 using same substrate is fully functional

## Slide 16: Micro SD Power Supplies
2 Step down power supplies
  1.2V, 1.8V
1 step up power supply
  3.3V from 2.7V
1 power supply monitor
  Detect under voltage

## Slide 17: Memory Stacking
LPDDR2
Nand x 2
Flash Ctrl
Flash Ctrl
LPDDR2
Nand x 2
LPDDR2
  Wirebonds N&S
Flash controller
  Wirebonds W
Nand Flash
  Wirebonds E
Total Thickness < 0.5mm
Total 250 wirebonds

## Slide 18: MPU on FPGA
FPGA
  Wire-bonds on 2 rows on 4 sides
  Die is smaller than MPU
  FPGA is under MPU
  191 Wire-bonds
MPU
  Wire-bonds on 2 rows on 4 sides
  Die is bigger than FPGA
  MPU is on top
  314 Wire-bonds
FPGA
MPU

## Slide 19: Linux on a Micro SD

## Slide 20: Conclusions
Design Process for Complex SiP has been demonstrated
Uses State of the Art « Mainstream » technologies
Avoids the use of expensive tool-sets
Avoids the use of unproven technologies
Heterogeneous SiP for medium volume requires a conservative approach
The Example micro SD SiP is probably smallest Linux computer today

## Slide 21: Thank you